Intec, Leipzig

Hall 3 / Stand F04/G05

Hall 2 / Stand B01

S224 cutting insert with internal cooling

The HP65-grade S224 cutting insert with internal cooling, featuring the 3V geometry in a 3 mm grooving width, is a new addition to the HORN range. Its wear-resistant AlTiN coating is specially designed for grooving and parting off stainless steels. The cutting insert with 3 mm cutting width and an internal coolant supply expands the areas of application that the cutting inserts from the S224 range have been suitable for up to now. The coolant jet acts directly on the cutting zone, thus ensuring optimum cutting conditions at this point. The funnel-shaped nozzle creates a coolant jet, which supports chip forming and thus reduces the chance of chip build-up. Furthermore, this type of internal cooling largely prevents the formation of built-up edges and break-outs on the cutting edge. Unlike conventional cooling methods, this system enable higher cutting parameters, which allow the tool to be used more cost-effectively. The square shank holder with internal cooling is available in dimensions of 16 x 16, 20 x 20 and 25 x 25 mm, in a right-hand and left-hand design. Coolant is transferred via a slot at the bottom. The holders are compatible with the relevant VDI supports and the screw clamping device for the cutting inserts benefits from a stop to allow inserts to be replaced easily with a high level of repeat accuracy.

1,376 characters incl. spaces

Image captions:

Image 1: Double-edged grooving insert with 3 mm cutting width and internal cooling

Image 2: Cooling through the double-edged grooving insert acts on the cutting zone

Image credits: Paul Horn GmbH, Nico Sauermann

Text and further information:

Hartmetall-Werkzeugfabrik Paul Horn GmbH, Mr Christian Thiele

Unter dem Holz 33-35, 72072 Tübingen, Germany

Tel.: +49 7071 7004-1602, Fax: +49 7071 72893

E-mail: christian.thiele@phorn.de, www.phorn.de